**Perovskite Solar Cells and Photocatalysis**

**Eric Wei-Guang Diau\*, Ming-Chou Chen, Chun-Hsiao Kuan**

aDepartment of Applied Chemistry, and Institute of Molecular Science National Yang Ming Chiao Tung University 1001 Ta-Hseuh Rd., Hsinchu 300093, Taiwan

E-mail: diau@nycu.edu.tw

**Abstract**

Tin-based perovskite solar cells (TPSCs) have emerged as promising alternatives to lead-based perovskites due to their lower toxicity, tunable optoelectronic properties, and potential for tandem applications. However, their commercial viability remains hindered by rapid oxidation of Sn²⁺, uncontrolled crystallization kinetics, phase segregation, and interfacial instability, which limit their efficiency and long-term stability, in particular to use PEDOT: PSS as HTL for TPSCs. To overcome these challenges, we have applied self-assembled monolayers (SAMs) to replace PEDOT:PSS using a two-step fabrication method developed by our group.1 The SAM molecules were designed to have a D-D-A structure, for which the head donor group (interacting with perovskite) is a triphenylamine (TPA) unit and the end acceptor group (anchoring on NiOx/ITO surface) is either -CN, -COOH, -PO3H2, or PO3E2 unit. The central donor group can be Thienopyrazine (TP) to attain PCE 7.7%,2 Y-shaped TPA to attain PCE 8.1%,3 Bithiophene Imide (BTI) to attain PCE, 8.6%,4 or I-shaped Selenophene (Sp) to attain PCE 8.7%.5 We will also present a PTAA-based all perovskite tandem solar cell to attain PCE 28.1%. A quadruple-cation mixed-halide TPSC with bandgap 1.93 eV to attain PCE 6.2% will be reported.6 On the other hand, photocatalytic CO2 reduction to generate CO will be presented with the photocatalysts of Zinc Indium Sulfide (ZIS),7 water-stable pseudohalide perovskites,8 and a S-scheme PeNC/BiVO4 heterojunction system.9 For water splitting, the H2 product yields were reported to give 17.1 mmol g-1 h-1 for Al-doped ZnS, 24.5 mmol g-1 h-1 for BiH4-modified SrTiO3 and 38.5 mmol g-1 h-1 for NH4Cl-modified K-PHI. Our promising results thus highlight the significance of using solar energies to produce electricity via efficient perovskite solar cells and solar fuels via efficient photocatalysts developed by our team.

**References**

1. S. Shahbazi, M.-Y. Li, A. Fathi and E. W.-G. Diau, ACS Energy Lett. **2020**, *5*, 2508-2511.
2. C.-H. Kuan, S. N. Afraj, Y.-L. Huang, A. Velusamy, C.-L. Liu, T.-Y. Su, X. Jiang, J.-M. Lin, M.-C. Chen and E. W.-G. Diau, *Angew. Chem. Int. Ed.* **2024**, e202407228.
3. S. N. Afraj,C.-H. Kuan,H.-L. Cheng,Y.-X. Wang,C.-L. Liu,Y.-S. Shih,J.-M. Lin,Y.-W. Tsai,M.-C. Chen and E. W.-G. Diau, *Small* **2025**, *21*, 2408638.
4. A. V., C.-H. Kuan, T.-C. Lin, Y.-S. Shih, C.-L. Liu, D.-Y. Zeng, Y.-G. Li, Y.-H. Wang, X. Jiang, M.-C. Chen and E. W.-G. Diau, *ACS Appl. Mater. Interfaces* **2025**, *17*, 953-962.
5. Y.-S. Shih, A. Velusamy, C.-H. Kuan, P.-Y. Huang, C.-H. Kuo, D.-Y. Zeng, C.-L. Liu, S.-H. Hong, X. Jiang, M.-C. Chen and E. W.-G. Diau, *Small* **2025**, *21*, 2500642.
6. I-. Tsai and E. W.-G. Diau, *Nanomaterials* **2024**, *14*, 1231.
7. C.-H. Kuan, Y.-C. Chen, S. Narra, C.-F. Chang, Y.-W. Tsai, J.-M. Lin, G.-R. Chen, and E. W.-G. Diau, *ACS Energy Lett.* **2024**, *9*, 2351−2357.
8. I-H. Tsai, C.-W. Huang, C.-F. Chang and E. W.-G. Diau, *Small* **2025**, *21*, 2409023.
9. I-H. Tsai, Y.-R. Kuo, H. Hiramatsu and E. W.-G. Diau, *J. Mater. Chem.* A **2025**, *13*, 6513-6523.